## Slide 1
The potential energy surface for catalytic reactions: an overview of computational catalysis
Michael Janik
Department of Chemical Engineering, Pennsylvania State University
mjanik@psu.edu
Mississippi State University
June 15, 2022

## Slide 2: Catalysis plays many roles in our energy future
Fossil fuel efficiency and diversification
-petroleum use efficiency
-methane to chemicals, liquid fuels
-coal to liquids
Flexible and efficient energy conversion
-Hydrogen production
-Electrocatalysis in fuel cells
-Electrolysis of CO2 for fuel production
Enable new energy feedstocks:
-biomass to fuels and chemicals
-renewable electricity to fuels
-solar fuels - photoelectrolysis
Notes: 2

## Slide 3
Catalyst activity and selectivity are controlled at the molecular scale:
Site composition
bimetallics, doped oxide
Structure and morphology
particle size, surface structure, defects, support interactions, stability
Surface interactions
coverage effects, intermolecular interactions, poisons, promoters
Reaction environment
temperature, pressure, solution, electric field
Notes: 3

## Slide 4
Explain at an atomic level what controls catalyst performance
First-principles guided catalyst design
Virtual lab: “computational experiments”
to design new catalytic materials
S. Trasatti. Electrochim. Acta 39 (1994) 1739.
B. E. Conway, G. Jerkiewicz. Solid State Ionics 152 (2002) 93.
HER
M-H binding energy (kJ/mol)
H2, gas  2H*
2H*  2H+ + 2e-
H2, gas 2H+ + 2e-
Catalyst 1
energy
rxn coordinate
Catalyst 2
Catalyst 3
H2(gas)
2H+(aq)+2e-
2H*
Catalyst Design Procedure:
Detailed studies on reaction steps, path, environment effects
Identify key parameters (energetics) that dictate performance
Evaluate parameters over a design space for improved performance

## Slide 5
Oxidation catalysis by metals: DFT for O2 activation
O2 molecular orbitals
O2 binding to metals and activation
Oxidation “volcano” curves
Notes: Add photos, revise text

## Slide 6
How does a metal catalyst activate O2 to participate in oxidation reactions?
Oxidation using molecular oxygen on metals
What is the key energetic parameter to dictate activity to reduce O2?
DFT calculation to first examine the electronic structure of O2
1) Build O2
2) Set-up geometry optimization calculation
3) DFT – solve for wavefunctions (orbitals), energy, minimum energy structure
4) Analyze results

## Slide 7
Geometry optimization of O2

## Slide 8
Geometry optimization of O2
1)Guess a distance: initial structure
dE/dx
2) DFT – get ’s, E, dE/dx
Move to new distance
Repeat until dE/dx ~ 0
Gives optimal structure and final E, ’s

## Slide 9
Geometry optimization of O2
O2 VASP energy = -9.823 eV
O VASP energy = -1.84 eV
Optimal bond distance 1.23 Å
Bond energy = E(O2)-2E(O)
= -6.15 eV = -593 kJ/mol

## Slide 10
O
O
2p
2p
2s
2s
2s*
2s
2p
2p*
x
y
x*
y*
O2
Molecular orbital diagram of O2
O—O bond distance 1.23 Å
O2 energy from VASP -9.82 eV Bond energy
O energy from VASP -1.84 eV E(O2)-2E(O) = -6.15 eV = -593 kJ/mol

## Slide 11
O
O
2p
2p
2s
2s
2s*
2s
2p
2p*
x
y
x*
y*
O2
Molecular orbital diagram of O2
O—O bond distance 1.23 Å
O2 energy from VASP -9.82 eV Bond energy
O energy from VASP -1.84 eV E(O2)-2E(O) = -6.15 eV = -593 kJ/mol

## Slide 12
Ground state (lowest energy electron occupation of orbitals) is a triplet
2 unpaired electrons in * orbitals.
O
O
2p
2p
2s

2s
O2
Molecular orbital diagram of O2







## Slide 13
Now I want to put O2 on a surface and calculate the energy change to adsorb it.
What DFT calculations do I need to run?
?
Notes: Might mention here – the dxz will have different energy, size, etc on different metals, bind O2 at different strengths, be better or worse at activating O2. Also, could mention Na promotion of O2 dissociation

## Slide 14
Now I want to put O2 on a surface and calculate the energy change to adsorb it.
What DFT calculations do I need to run?
O2(gas) + surface  O2 on the surface
Eads = EO2 on surface – EO2 in gas phase – Esurface with nothing on it
DFT calculations
O2 gas
Surface (*)
O2 on surface (O2*)
O2 + *  O2*
Notes: Might mention here – the dxz will have different energy, size, etc on different metals, bind O2 at different strengths, be better or worse at activating O2. Also, could mention Na promotion of O2 dissociation

## Slide 15
Woody will show you how to build (cut) a surface later today, and how to put an adsorbate on that surface.
Let’s take a look at O2 on a surface.
Choices – how many layers?
What is frozen?
What is my supercell size (I am showing you a 3x3 surface cell – 9 Pt atoms per layer). Surface cell size dictates “fractional coverage”
Notes: Might mention here – the dxz will have different energy, size, etc on different metals, bind O2 at different strengths, be better or worse at activating O2. Also, could mention Na promotion of O2 dissociation

## Slide 16
O2 on metal surface – bonding is between O2 * orbital and metal d orbitals
O
O
M
O2 *
M dxz
O2 * and M dxz form a bonding orbital
Occupation lowers energy – O2 has an exothermic adsorption
E(O2) = -9.823 eV
E(Pt(111)) = -315.201 eV
E(O2 on Pt(111)) = -325.624 eV
Adsorption energy = -0.60 eV = 58 kJ/mol
O2 *
M dxz



Donation of e- from M dxz to O2 * orbital weakens O—O bond, lowering bond dissociation barrier
(O—O gas 1.23 Å, O—O on Pt(111) 1.37 Å)
Notes: Might mention here – the dxz will have different energy, size, etc on different metals, bind O2 at different strengths, be better or worse at activating O2. Also, could mention Na promotion of O2 dissociation

## Slide 17
Potential energy surface of O2 activation on metals
We can connect the O2 dissociation barrier and resultant rate to the extent of electron donation to the O2 * orbital
Catalyst 1
energy
rxn coordinate
Catalyst 2
Catalyst 3
H2(gas)
2H+(aq)+2e-
2H*
O2+*
O2*
2O*
No catalyst, Eact = 6.15 eV
0.57
eV
1.90
Au(111)1
Pt(111)
Na
-
O—O
+
e-
0.40
1) Au(111) data from Fajin et al. Applied Catalysis A: General 458 (2013) 90
Notes: PES should have gas phase barrier, Pt(111) barrier, Pt-Na-111 barrier.

## Slide 18
What DFT calculations did I have to run to map out the “potential energy” surface on the last slide?
?
Notes: Might mention here – the dxz will have different energy, size, etc on different metals, bind O2 at different strengths, be better or worse at activating O2. Also, could mention Na promotion of O2 dissociation

## Slide 19
What DFT calculations did I have to run to map out the “potential energy” surface on the last slide?
O2 gas phase
*
O2*
2O* (ie, the product state for O2 molecule dissociating)
A transition state search for the highest energy state as the O-O bond stretched to become 2 O
Notes: Might mention here – the dxz will have different energy, size, etc on different metals, bind O2 at different strengths, be better or worse at activating O2. Also, could mention Na promotion of O2 dissociation

## Slide 20
If O2 activates easier (more quickly) than O binds more strongly.
Note same pattern for other diatomics (N2, CO, NO)
Product adsorption strength
Dissociation activation barrier
1) Figure from Bligaard et al., J. Catal. 224 (2004) 206
Faster O2 activation correlates with stronger O binding
Notes: PES should have gas phase barrier, Pt(111) barrier, Pt-Na-111 barrier.

## Slide 21
Oxygen reduction reaction (proton oxidation reaction)
O2 + H2  O or OH intermediates  H2O
Optimal catalyst has an intermediate binding energy for oxygen
Sabatier’s principle: optimal rate occurs with medium binding reaction intermediate
Reaction rate
Left figure from Bligaard et al., J. Catal. 224 (2004) 206; right figure from Zhang et al., Angew Chemie 44 (2005) 2132
Pt(ML) on M(111)
Pt/Pd(111)
Pt (111)

## Slide 22
DFT can give us remarkably detailed and accurate insight
Electronic structure nature of
O2 * - Metal d interaction
Elementary reaction energetics
(activation barriers)
Correlations across reaction steps
in a mechanism
Catalyst material optimization
Notes: PES should have gas phase barrier, Pt(111) barrier, Pt-Na-111 barrier.

## Slide 23: Reaction Intermediates and Adsorption Sites
BO2*
(+6H2O+8e-)
BH4* (+8OH-)
BH3OH*
BO2*
BOOH*
BH*
BH2*
BH2OH*
BHO*
B(OH)2*
BH3*
BHOOH*
BO*
BOH*
BH4*
H*
BH2O*
BH(OH)2*
Assumption – all adsorbates can access there most stable configuration

## Slide 24
Minimum Energy Path over Au(111)
Relative energy (eV)
Borohydride oxidation
0.0
-1.0
-2.0
-3.0
-4.0
-5.0
-6.0
-7.0
BH2*
BH2OH *
BHOH*
BO2*
BOOH*
B(OH)2*
U= -1.0 V (NHE)
BH(OH)2*
BH3*
1.0
BH4- (aq)
BH4*
BH2OH*
BH(OH)2*
BH4*
BH3*
BH2*
BHOH*
B(OH)2*
BOOH*
BO2*
U= -0.2 V (NHE)